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Cable type: AAC 66-AL1 Standard: EN 50182

p05

All Aluminium Conductor (AAC) is concentrically stranded conductor with one or -~
more layers of hard drawn aluminium wires.

Characteristic Unit Value
Number of wires pes. 19
Diameter of wire mm 21
Diameter of conductor mm 10,5
Conductor cross section mm’ 65,8
Weight of conductor ke/km 180,9
Lowest laying temperature c -20
Conductor DC resistance per km at 20°C Ohm/km <0,4367
Maximum permissible duration of short dircuit B 5
Maximum permissible continuous conductor temperature - 80
Maximum permissible conductor temperature during the short circuit C 160
Rated strength kN 211,85
Final modulus of elasticity N/mm 57000
Coefficient of linear expansion /K 2,30E-05
Delivery length per drum m 2500
Gross weight of full cable drum kg 552
Diameter of cable drum mm 1220
Width of cable drum mm 500
Manufacturers name Energocomplekt





